CARACTERÍSTICAS DO PRODUTO:

ARAME TUBULAR

REVESTIMENTO DURO

ESSEN MS 69 B

Classifications: AWS A5.5:2014E9018- D1 ASME SFA5.5 E9018-D1

E9018-D1 – Basic coated electrode

Special low-alloy electrode for welding heat-resistant steels and similar structures, suitable for various industries. Intended for restoration and protective overlay against wear, offering easy slag removal, high deposited metal yield, and excellent impact toughness.

| ALLOY TYPE: |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| C 0,12% Máx. | Mn 1,00% a 1,75% | Si 0,80% Máx. | P 0,030% Máx. | S 0,030% Máx. | Ni 0,90% Máx. | Mo 0,25% a 0,45% |

| MECHANICAL PROPERTIES: |  |  |  |
| --- | --- | --- | --- |
| TENSILE STRENGTH: | YIELD STRENGTH: | ELONGATION: | IMPACT RESISTANCE: |
| 620 MPa (min) | 530 MPa | 17% (min) | 27J-50°C |

| WELDING CURRENT: | CC+; CA |
| --- | --- |
| COATING TYPE: | BASIC |

Plana             Horizontal            Vertical               Sobre Cabeça

CARACTERÍSTICAS DO PRODUTO:

| CARACTERÍSTICAS DO PRODUTO: |  |  |  |
| --- | --- | --- | --- |
| DIAMETER (mm): | LENGTH (mm): | AMPERAGE (A): | PACKAGING (kg): |
| Ø 2.50 | 350 | 60 a 100 | 5.00 |
| Ø 3.25 | 350 | 110 a 140 | 5.00 |
| Ø 4.00 | 450 | 140 a 180 | 5.00 |
| Ø 5.00 | 450 | 180 a 220 | 5.00 |

CARACTERÍSTICAS DO PRODUTO:

CARACTERÍSTICAS DO PRODUTO:

CUSTOMER SERVICE POLICY

The information above is provided for reference purposes only and should not be considered as a guarantee or certification. Many variables can influence the results of a welding operation. Uniweld Indústria de Eletrodos LTDA is not responsible for any incorrect application of the product. If you have any questions, we recommend contacting our Technical Assistance department for proper support.